## Slide 1
LAMINATE FLOORING
SPOTTED GUM
Structure | HDF Base Material
Size | 2200*196*12 mm
Pack Size | 2.156sqm/pack
Profile | Click System
Finish | Gloss, Water Resistance
Edge | Micro Bevel
Installation Method | Floating
Fire Test CHF Value | Mean 7.0 kW/m² (AS/ISO 9239.1-2003)
Fire Test Smoke Value | Mean 11% min (AS/ISO 9239.1-2003)
Wear Layer Domestic Warranty | 5 Years
Structural Domestic Warranty | 25 Years
Disclaimer
Product baches, variations can occur between samples, in showroom displays and printed and online imagery. Please ensure you review your sales order and the actual product PRIOR to your flooring being installed as although we endeavor to represent our products to the best of our ability this natural variation can cause differences.